## Slide 1: Irradiation of polymer foil using single MeV-energy heavy ions
Laboratory for ion beam interactions
Ruđer Bošković Institute
Nora Reinić
Supervisor: Georgios Provatas
Seminar in Research in Physics
a.y. 2021/22

## Slide 2
Brief summary of the experiment
1. Irradiation of the foil with single ions from the ion beam
Ions pass through the foil and create permanent damage
2. Chemical etching
FINAL PRODUCT:
a foil with μm-sized pores arranged in rectangular pattern
polymer foil
ion
Ion beam
Etching enchances that damage

## Slide 3
Specifically in polymers:
electron collisions can cause breaking or linking of the long chain molecules
What happens when an ion passes through a dielectric solid?
Theoretical background
1.
2.
3.
4.
s
s
Electron collision cascade
Relaxation of defects
s
A cylindrically shaped track core is formed
s
A region full of point defects!
Direct ion-target interaction
Coulomb explosion
- the defects tend to aggregate along the ion’s trajectory
Atomic collision cascade

## Slide 4
Theoretical background
latent tracks – permanent tracks of aggregated defects
radial cut through a track:
TRACK CORE
atomic collision cascade
CHEMICALLY ACTIVE REGION
specific for polymers
TRACK HALO
electronic collision cascade
10 nm
100 nm
1000 nm

## Slide 5
Theoretical background
How do we know if an ion will create latent tracks?
Important quantity:
= energy loss per unit length of path, dE/dx
Nuclear stopping power – ion-nuclei interactions
Electronic stopping power – ion-electron interactions
STOPPING POWER
dominant for small ion energies
causing abrupt changes in ion’s trajectory
causes only short tracks because the ion stops very soon
dominant for large ion energies
slows down the ion smoothly
can cause formation of latent tracks
nuclear
electronic

## Slide 6
Theoretical background
Electronic stopping power curves computed with SRIM software
we need heavy ions of MeV energies!

## Slide 7
Theoretical background
The latent tracks are too small, what do we do?
CHEMICAL ETCHING
Chemically very active regions!
nm
μm
Immersing the irradiated material in a suitable solution triggers the chemical reactions along the latent track
the damaged
zones get disolved
KOH/NaOH
POLYMERS: the damaged area extends radially further in comparison to other dielectrics
ideal for etching

## Slide 8
Experimental method
Ruđer Bošković Institute – Laboratory for ion beam interactions
There are two (and one more in the making)
tandem accelerators in the facility
multiple experimental beam lines with different purposes
ion source
6.0 MV EN Tandem Van de Graaf accelerator
in reality this is not a straight line, there are magnets directing the beam
accelerator
ion microprobe

## Slide 9
Experimental method
Ion microprobe
Two operational modes:
HIGH CURRENT MODE
1-1000 pA
LOW CURRENT MODE
< 1 fA
Scanning pattern:
detectors
32 x 32

## Slide 10
Experimental method
Transmitted ion triggers the detector
Tells the beam scanner to switch to the next position
It takes a few seconds to scan the entire area
Target chamber
Beam scanner

## Slide 11
Experimental method
How do we know the ions will pass through the foil, not stop in it?
SRIM software
Input:
ion species and energy
target composition and width
Output:
simulations of the ion target interactions
stopping ranges
stopping power
20 MeV carbon ions
6 μm thin polycarbonate foil
+
We used:
Stopping ranges for different ion species

## Slide 12
Experimental method
Chemical etching recipe
200 mL KOH solution (n = 3 mol/L)
heat to 50 °C
put the foil in the solution for 40 min
After the etching, the foil was left to dry for several days and then examined with optical microscope

## Slide 13
Results
We irradiated 6 spots on a foil with different
scanning parameters:
Scanned area dimensions:
(213 ± 5) μm
or
(426 ± 5) μm
Number of ions per spot:
1 ion/spot
or
2 ions/spot
Order of scanning:
or
longer side length
Finding the pores with optical microscope – wasn’t easy
Foil diameter:
1.5 cm
Irradiated area surface:
< 1 x 1 mm2
folds on foil
+
other minor damages on the foil surface
+

## Slide 14
Results
10x
10x
40x
60x
10 μm
10 μm
5 μm

## Slide 15
Conclusion
The results are satysfactory
- we succesully created the pores and they were arranged in a regular pattern
Possible improvements:
each irradiated area should be marked during the scanning with, for example,
a bigger, easily noticeable damage focused next to it
even the very small damages of the foil surface are clearly visible under the microscope
be more careful with handling the foil, trying to minimize the contact with the surrounding surfaces
small folds significantly
alter the image under the microscope
more care should be devoted to fixating and stretching the
foil over a sample holder
it could not be recognized
which of the observed pores correspond to which of the six scanned regions.
use heavier ions for bigger irradiation damage and better defined pores

## Slide 16
The end
Thank you for attention!